## Slide 1
Controlled Self-assembly of Colloidal Cobalt Nanocrystals
Yuping Bao, Michael Beerman and Kannan M. Krishnan
Cobalt Nanocrystals Synthesis
BF TEM image of 10nm Cobalt sphere and 520nm nanodics
We demonstrate the possibility of obtaining a rich set of self-assembled arrays from a single component cobalt nanocrystal (NC) system by a controlled variation of size, shape and inter-particle interactions. By selecting appropriate conditions in which one of a set of weak but competing interaction forces (steric, van der Waals, depletion, or magnetostatic) dominates, we can reproducibly achieve a wide range of nanocrystal arrays. This includes hexagonal and square arrays, arrays spatially segregated by size, linear chains and lyotropic crystals exhibiting increased orientation order as a function of concentration.
ABSTRACT
Self-assembly of 8-10 nm Co nanocrystals
Hexagonal close-packed 2D lattice of 8-10 nm spherical nanocrystals. a) TEM image
b) XRD -2 scan, peaks correlate with -cobalt c) Closed hysteresis loop indicates superparamagnetic behavior.
In this case, a hard-sphere model applies and the hexagonal arrangement results from a first order phase transition as a function of concentration.
Self-organization Behavior of Cobalt Nanocrystals as a Function of Size and Shape
Self-assembly of very small 4 nm Co nanocrystals
Two dimensional square lattice of 4nm spherical nanocrystals. a) TEM image b) XRD -2 scan showing size effect peak broadening, but peak position indicates -cobalt c) Closed hysteresis loop suggests superparamagnetic behavior.
The hard-sphere model breaks down, leading to significant surfactant overlap. A square arrangement minimizes the overlap volume and dominates the self-assembly process.
Self-assembly of Bimodal size distributions
TEM images of nanocrystals with non-uniform size distributions. a) spherical nanocrystals
b) nanodisks – the shape of the nanocrystals were confirmed independently by tilting and high resolution electron microscopy.
In this case the entropy-driven depletion force dominates leading to a spatial separation as a function of size. Note that this is independent of the shape of the nanocrystals.
Self Assembly of 18nm Co Nanoparticles
Chains of 18-20 nm spherical nanocrystals. a) TEM image b) XRD -2 scan, peaks correlate with -cobalt c) Open hysteresis loop suggests ferromagnetic behavior.
The magnetostatic interaction between ferromagnetic particles determines the self-assembly.
Self Assembly of Co Nanodisks: Lyotropic Liquid Crystals
Arrays of nanodisks (5nm thick, 20 nm diameter).a, b) TEM images. Orientation order increases with concentration, i.e. lyotropic liquid crystal behavior. c) XRD -2 scan, peaks correlate with hcp cobalt d) Open hysteresis loop suggests ferromagnetic behavior.
The magnetostatic energy is a minimum when the neighboring disks lie face to face.
ABSTRACT
In summary, we have demonstrated that a rich set of self-assembled arrays can be obtained from a single component system by a controlled variation of nanocrystal size, shape and inter-particle interactions. Moreover, in a nanocrystal system in which a number of weak but competing interaction forces exist, by selecting appropriate conditions in which one of them dominates we can achieve significant control and diversity in the nature of the self-assembled arrays. This principle could serve as a fundamental guideline for the controlled self-assembly of nanoparticle arrays with implications for emerging photonic, magnetic and electronic applications, such as data storage and spin electronics. We are studying large area self-assembly by SAXS and magnetic interaction with Electron Holography. The primary results show that large area self-assembly have uniform particle size distribution and interaprticle distance and the magnetic coupling between the large size particles.
Acknowledgements:
This work is funded by NSF (DMR-0203069) and the Campbell Endowment at UW. YB acknowledges a PNNL-UW JIN and UIF nanoscience fellowship.
CONCLUSION
Self-assembly Technique
Evaporation rate gradient technique is developed to assemble Cobalt nanocrystals,in which mixtures of solvents (toluene, hexane, dichlorobenzene) and non-solvents (methanol, butanol) with different boiling temperatures produce an evaporation rate gradient. This technique allows particles to remain in solution with sufficient thermal energy to slowly form highly ordered structures. The non-solvent mixture is added drop wise to a dilute solution of particles, which precipitate onto a SiO or amorphous carbon TEM film. This method produces 2D arrays most of the time .
University of Washington
Contact Information
http://depts.washington.edu/kkgroup or email at:
Kannan M. Krishnan kannanmk@u.washington.edu
Yuping Bao baoyp@u.washington.edu
Reference:
1.Y.Bao, M.Beermen, K.M.Krishan, JMMM (inpress)
2.V.Puntes et, al . Science291(2001) 2115
3. For more information about magnetic measurement see poster:
Low temperature magnetization behavior of epsilon-cobalt nanosphere system
2-vpm29 location F
La Mer & Dinegar, J.Am. Chem. Soc. (1950)
Murray, Kagan and Bawendi, Ann. Rev. Mat. Sci.(2000)