## Slide 1
Ion-beam Sputtering Deposition
Vacuum System
Thickness
Monitor
Substrate
Heater (1000°C)
Kaufman
Ion Gun
Multiple
Target
Holder
Ar
Cathode
Anode
Glow
Discharge
Magnets
3 cm focused
0.25-1.25 kV
20-50 mA
0.1-1.0 Å/sec dep. rate
Load
Lock
Substrate: MgO(001)
4.2Å
Ferromagnet: Fe (001)
2.86Å
Antiferromagnet: MnPd (001)
4.07Å
Capping layer: Au
In-plane epitaxial relationship: [100]MgO || [110]Fe || [100]MnPd
Thin Film Architecture
Structural Characterization - X-Ray Diffraction
High-Angle XRD Scan
Sensitive to crystalline structure
Au30Å/MnPd450Å/Fe50Å/MgO(001) Substrate temperature: ~ 400ºC
Low-Angle Reflectivity Scan
Sensitive to interface roughness
and layer thicknesses
The MnPd film is is mainly c-axis oriented containing some a-axis orientated grains
Texture scan of Fe (220)
Note : Rotation by 45° w.r.t. MnPd
X-ray Diffraction - Texture Scans
Texture scan of MnPd (202)
Pure c-axis orientation, no a-axis component
~ 500ºC
Texture scan of MnPd (202)
c-axis oriented (main component) plus an a-axis oriented component
~ 400ºC
High growth temperature is critical to achieve high quality films
Epitaxial growth and exchange biasing of FM/AFM bilayers
Normal
Structure
PdMn (~280Å)
Fe (~60Å)
MgO(001)
10
20
30
40
50
60
70
80
Intensity (arb. units)
2Theta
a-growth
(002)MgO
(200)MnPd
(004)Fe
-0.8
0
0.8
-500
0
500
Moment(memu)
H(Oe)
He= 9 Oe
10
20
30
40
50
60
70
80
(001)MnPd
(002)MnPd
(002)MgO
(004)Fe
c-growth
-0.5
0
0.5
-500
0
500
Moment(memu)
H(Oe)
He = 30 Oe
a-axis normal
3.58Å
4.07Å
4.07Å
Spin Uncompensated
3.58Å
4.07Å
4.07Å
c-axis normal
Spin Compensated
Intensity (arb. units)
PdMn/Fe/MgO - Summary of growth & magnetic properties
-10
0
10
20
30
40
0
100
200
300
400
500
He (Oe)
Growth Temperature (°C)
Annealed
As-grown
a-axis growth
c-axis growth
Disordered
Ordered
Total energy:
E = -HMcos(-)- K1cos()
+ K2sin2() + K3sin2()cos2()
K1=Unidirectional Fit => 2.9E5 erg/cm3
K2=Uniaxial Fit => 0
K3=Cubic Fit => 4.5E5 erg/cm3
bias
M
H


Torque magnetometry
Field: 1000 Oe
Anisotropy modeling
Fe (100)//bias//H
Fe (010)
Fe (110)
Fe (-110)
The path that the magnetic moments follow when the magnetic field is changed is given by the arrows
Magnetization process: α = 0
Fe (010)
Fe (110)
Fe (100)//bias
Fe (1-10)//H
Magnetization process: α = 45
Fe (0-10)//H
Fe (1-10)
Fe (100)//bias
Fe (110)
Magnetization process: α = 90
Above 450 - 500ºC interdiffusion between the MnPd and Fe layer is initiated. The magnitude of the bias decreases while the coercivity increases dramatically.
Low-angle reflectivity scan => Interface roughness ~ 12 Å
α = 0
α=45
α=90
Effect of growth temperature - Interdiffusion
Exchange coupling in nanoscale MnPd/Fe heterostructures
Peter Blomqvist and Kannan M. Krishnan
University of Washington, Materials Science and Engineering Department, 302 Roberts Hall, Seattle, WA 98195-2120, USA
The MnPd/Fe interface roughness is roughly 2.5 Å, i.e. about two atomic monolayers
Acknowledgements:
This work was supported by DoE Materials Science Division under grant # DE-FG03-02ER45987 and by the Campbell Endowment at UW.
We would like to thank David E. McCready at the EMSL/Pacific Northwest National Laboratory for the help with the XRD measurements and Erol Girt, Seagate Technology Inc., for the help with the torque measurements.
For more information, please visit our website at http://depts.washington.edu/kkgroup/
ABSTRACT
The magnetization process in an exchange biased MnPd/Fe bilayer has been investigated using vibrating sample and torque magnetometry. A simple analytical model based on coherent magnetic moment rotation was used to qualitatively explain and describe the magnetization process. The shift of the hysteresis loop, the increased coercivity, the easy and hard axis behavior as well as the intermediate magnetic state seen in the hysteresis loops are reproduced in the model. However, the magnitude of the bias and the coercivity are not strickly in agreement with the measured values. The discrepancies are attributed to the simplified model which does not take into account the role of magnetic domains or disorder at the MnPd/Fe interface.
Submitted to Applied Physics Letters
Journal of Applied Physics 89, 6597 (2001)